### 750 SS Welding Blanket

Heavy-Duty Woven Fabric for Welding Protection and Fire Safety

750 SS Welding Blanket is a heavy-duty fabric woven from high SiO₂ content yarn (≥96%) and treated with a specially formulated acid process. This silica cloth is suitable for continuous service at 1100°C (2000°F) and can withstand short-term exposure up to 1400°C (2550°F).

The fabric is available with optional Polyurethane or Vermiculite coatings, which enhance abrasion resistance and tensile strength. It is ideal for heat preservation applications, firefighting equipment, fire curtains, welding blankets, fireproof garments, and high-temperature filtration systems. Style 750 SS is also widely used for manufacturing preformed fire and welding blankets with fiberglass tape edging and brass eyelets.

### Key Features

● Manufactured from high SiO₂ content yarn (≥96%) for superior thermal performance.

● Suitable for continuous operation at temperatures up to 1100°C and short-term exposure up to 1400°C.

● Available with Polyurethane or Vermiculite coatings for enhanced abrasion resistance and durability.

● Satin weave construction provides excellent flexibility and mechanical strength.

● Offers outstanding resistance to thermal shock and extreme heat exposure.

● Suitable for use in high-temperature filtration and molten metal processing applications.

### Applications

● Welding blankets and welding curtains.

● Fire curtains and fireproof safety equipment.

● Fireproof garments and thermal protection systems.

● Heat preservation and insulation applications.

● High-temperature dust collection and filtration systems.

● Molten metal filtration and industrial heat shielding applications.

### Technical Specifications

| Property | Value |
| --- | --- |
| Weave | Satin 8HS / 12HS |
| SiO₂ Content | ≥ 96% |
| Service Temperature | 1100°C (2000°F) |
| Maximum Temperature | 1400°C (2550°F) |
| Melting Temperature | 1800°C (3270°F) |
| Linear Shrinkage (1000°C, 30 Min) | < 7.10% Max. |
| Area Shrinkage (1000°C, 30 Min) | < 13% Max. |
| Weight | 600 g/m² (0.7 mm Thick) / 1150 g/m² (1.4 mm Thick) |
| Tensile Strength (Warp) | ≥ 800 N/Inch / 1100 N/Inch |
| Tensile Strength (Weft) | ≥ 600 N/Inch / 900 N/Inch |
| Thread Count (Warp) | 20 per cm |
| Thread Count (Weft) | 15 per cm |
| Color | White / Golden |
| Available Sizes | Width 900 to 1000 mm |
| Thickness Options | 0.7 mm & 1.4 mm |

### Performance Benefits

● Continuous service capability up to 1100°C with short-term exposure up to 1400°C.

● High silica content provides excellent thermal stability and fire resistance.

● Available coating options improve abrasion resistance and service life.

● Excellent tensile strength ensures durability in demanding industrial environments.

● Provides both thermal and electrical insulation for enhanced operational safety.

● UL-94 V0 certified for fire-resistant applications.

● Suitable for extreme-temperature environments requiring reliable thermal protection.

This is the exact format I'll follow for the remaining datasheets.