CG 102

Engineered for Extreme Conditions – Reliable Sealing with Advanced Graphite Technology

Style CG 102

INMARCO Style CG 102 is manufactured from premium expanded graphite yarn containing a minimum of 98% carbon content and reinforced with resilient Inconel wire. The packing is impregnated with a proprietary graphite-based dispersion and a corrosion inhibitor system that protects equipment against galvanic corrosion while enhancing sealing performance in demanding applications.

The flexible Inconel wire reinforcement provides excellent mechanical strength and pressure resistance, while the self-lubricating graphite structure assists stem adjustment during gland tightening. The advanced graphite-based lubricant minimizes leakage in both static and dynamic equipment, making Style CG 102 an ideal solution for valves, autoclaves, rotary kilns, and other high-temperature sealing applications.

KEY FEATURES

● Manufactured from premium expanded graphite yarn with a minimum carbon content of 98%.

● Provides excellent thermal conductivity and chemical resistance across a broad range of industrial media.

● Reinforced with strong yet flexible Inconel wire for superior structural integrity under pressure and temperature fluctuations.

● Optional multi-wire reinforcement is available for enhanced resistance to pressure surges and severe operating conditions.

● Proprietary graphite-based dispersion improves sealability and minimizes leakage.

● Self-lubricating graphite structure allows smooth stem adjustment during gland tightening.

● Integrated corrosion inhibitor system protects equipment against galvanic corrosion and pitting.

● Chemically inert and suitable for applications where media contamination must be avoided.

APPLICATIONS

● Industrial valves.

● Autoclaves.

● Rotary kilns.

● Steam systems.

● Hydrocarbon processing equipment.

● Thermic fluid systems.

● Hot oil applications.

● Cooling water systems.

● Rotary and rising-stem valve applications.

TECHNICAL SPECIFICATIONS

| Property | Value |
| --- | --- |
| pH Range | 0 – 14 |
| Temperature Range | -240°C to +538°C |
| Pressure Rating | 300 bar |
| Available Sizes | 6.5 sq mm to 50 sq mm |
| Construction | Expanded Graphite Yarn with Inconel Wire Reinforcement |
| Carbon Content | Minimum 98% |

PERFORMANCE BENEFITS

● Exceptional high-temperature resistance up to 3000°C in non-oxidizing environments.

● Low oxidation characteristics provide extended service life under extreme thermal conditions.

● Fire-safe design suitable for critical industrial and fire-rated applications.

● Inconel wire reinforcement delivers outstanding pressure resistance and mechanical stability.

● Self-lubricating graphite reduces friction and wear during operation.

● Corrosion inhibitor system protects valve stems and equipment from galvanic corrosion.

● Excellent thermal conductivity promotes efficient heat dissipation and cooler operation.

● Suitable for rotary and rising-stem valve applications from Class 150 to Class 1500.

● Maintains sealing integrity under high pressure and severe operating conditions.

● Provides long-term reliability in steam, hydrocarbon, thermic fluid, and hot oil services.

ADDITIONAL INFORMATION

● Optional multi-wire Inconel reinforcement is available for applications requiring enhanced surge resistance.

● For valve classes above Class 1500, please consult INMARCO Technical Services.

s