# FG 320

## Flexible Pure Graphite Sheet for High-Temperature and High-Pressure Sealing

FG 320 is manufactured from exfoliated graphite. During the initial exfoliation process, graphite undergoes acid treatment; however, all residual acids are thoroughly removed using demineralized (DM) water. The subsequent manufacturing process is entirely mechanical and does not involve the addition of binders, fillers, oils, or other additives.

The sheet consists of 99% pure carbon graphite, providing exceptional sealing performance in demanding high-temperature and high-pressure applications. Its highly resilient structure enables it to conform to flange irregularities and surface imperfections, ensuring reliable sealing performance.

FG 320 is suitable for use with metallic, glass, and enamel flanges and is designed to facilitate easy maintenance and gasket replacement. The material remains dimensionally stable under pressure fluctuations and is also suitable for cryogenic services.

## Key Features

● Manufactured from high-purity exfoliated graphite with 99%carbon content.

● Free from binders, fillers, oils, and other additives.

● Excellent resistance to high temperatures and high pressures.

● Highly resilient and adaptable to flange surface irregularities.

● Dimensionally stable under extreme pressure surges.

● Suitable for cryogenic as well as elevated temperature applications.

● Excellent chemical resistance across a broad range of industrial media.

● Compatible with metallic, glass, and enamel flanges.

## Applications

● Pipe flanges

● Valve bonnets

● Heat exchangers

● High-temperature process equipment

● Cryogenic systems

● Industrial sealing applications requiring high chemical resistance

## Service Media

● Superheated and saturated steam

● Non-oxidizing liquids and gases

● Hydrocarbons

● Oxygen service

● Cryogenic fluids

● Dyes and chemicals

● Acids (except hydrofluoric acid)

● Alkalis

● Fuel oils and lubricating oils

## Technical Specifications

### Operational Parameters

| Property | Value |
| --- | --- |
| pH Range | 0 – 14 |
| Temperature (°C) | -200 to +550 |
| Pressure (Bar) | 150 |
| Thickness (mm) | 0.5 – 6 |

### Material Properties

| Property | Value |
| --- | --- |
| Carbon Content | 99% |
| Sulphur Content | < 750 ppm |
| Chloride Content | < 45 ppm |
| Ash Content | < 1% |
| Density Tolerance | ±0.05 g/cc |
| Sheet Thickness | 0.5 mm – 6 mm |
| Thickness Tolerance | ±0.1 mm to ±0.25 mm |

### ASTM F36

| Property | Value |
| --- | --- |
| Compressibility | 35 – 40% |
| Recovery | 15 – 18% |
| m Factor (3 mm Thick) | 2.5 |
| y Factor | 2176 psi |

### ASTM F38

| Property | Value |
| --- | --- |
| Creep Relaxation | 5% |

### Ignition Loss

| Temperature | Value |
| --- | --- |
| 454°C (850°F) | 1% |

### Extended Service Limits

| Property | Value |
| --- | --- |
| Temperature (Reducing Atmosphere) | Up to 3000°C |
| Temperature (Oxidizing Atmosphere) | Up to 480°C |
| Temperature (Steam Service) | Up to 550°C |
| Pressure | Vacuum to 150 Bar |

## Availability

### Sheet Sizes

● 1000 mm × 1000 mm

● 1500 mm × 1500 mm

### Thickness Range

● 0.5 mm to 6 mm

## Performance Benefits

● Exceptional sealing performance under high temperatures and pressures.

● Conforms readily to flange irregularities, reducing leakage risk.

● Excellent resistance to thermal cycling and pressure fluctuations.

● Chemically resistant to most industrial fluids and gases.

● Suitable for both high-temperature and cryogenic services.

● Dimensionally stable with minimal creep and relaxation.

● Low leakage rates ensure reliable long-term sealing.

● Reduces maintenance frequency and overall operating costs.