# HY 105HD

### Designed for Critical Applications in Urea and Ammonia Systems

## 1. PRODUCT OVERVIEW

INMARCO HY 105HD is a dense braided gland packing manufactured with Aramid Yarn corners and PTFE Yarn faces, reinforced by a high-tensile Aramid fibre core for superior strength and dimensional stability, preformed and compressed under heavy load. It is specifically designed for high-pressure and high-temperature applications where reliable sealing performance is critical.

This high-density packing is widely used in fertilizer industry applications involving ammonia, urea, and carbamate services. The Aramid yarn is treated with antifriction fluoropolymer and break-in lubricant, while the PTFE faces are lubricated with inert high-temperature-resistant compounds. This combination ensures low friction, reduced equipment wear, and long operational life.

## 2. KEY FEATURES

● High-density braided construction provides excellent sealability and dimensional stability under severe operating conditions.

● Aramid Yarn corners provide superior structural strength and resistance to corner failures.

● PTFE Yarn faces offer low friction characteristics and cooler shaft operation.

● Reinforced with a high-tensile Aramid fiber core for enhanced mechanical strength.

● Aramid fibers are treated with antifrictional fluoropolymer and break-in lubricant for smooth operation.

● PTFE faces are lubricated with inert high-temperature-resistant compounds.

● Excellent resistance to ammonia, urea, carbamate condensate, detergents, pigments, and synthetic molten materials.

● Reduces wear on plungers, valve stems, and rotating equipment.

## 3. APPLICATIONS

● Reciprocating pumps

● Plunger pumps

● Agitators

● Mixers

● Extruders

● Reactors

● Fertilizer plants

● Urea processing units

● Ammonia handling systems

● Carbamate processing equipment

## 4. TECHNICAL SPECIFICATIONS

### Technical Properties

| Property | Reciprocating |
| --- | --- |
| pH Range | 0 – 14 |
| Temperature Range | -200°C to +300°C |
| Pressure (Bar) | 200 |
| Velocity (m/s) | 10 |
| Available Sizes | 3 sq mm to 35 sq mm |

## 5. SERVICE MEDIA

● Ammonia

● Urea

● Carbamate condensate

● Detergents

● Pigments

● Synthetic molten materials

● Fertilizer process chemicals

● Industrial process fluids

## 6. PERFORMANCE BENEFITS

● Exceptional high-pressure resistance due to the strong Aramid fiber core.

● Low-friction PTFE faces ensure cool shaft operation and reduced wear.

● High-density braided construction provides superior sealability and dimensional stability.

● Wide chemical compatibility including ammonia, urea, and carbamate solutions.

● Suitable for reciprocating, centrifugal, and plunger pumps used in fertilizer applications.

● Operates effectively across a wide temperature range from -200°C to +300°C.

● Designed specifically for critical fertilizer industry applications requiring reliable sealing performance.

● Excellent resistance to mechanical wear and extrusion.

● Reduces maintenance frequency and extends equipment service life.

● Provides dependable sealing performance under demanding operating conditions.

## 7. INDUSTRY APPLICATIONS

● Fertilizer Plants

● Ammonia Production Units

● Urea Processing Facilities

● Chemical Processing Plants

● Petrochemical Facilities

● Process Industries Handling Aggressive Media

### 7. COMPLIANCE

- FDA Certified