## 1. PRODUCT OVERVIEW

INMARCO HY 107 is a unique multi-yarn packing specifically designed for harsh industrial sealing applications. The packing combines Aramid filament yarn at the corners with graphite-lubricated PTFE yarn on the sealing faces and an Aramid filament core. The packing is performed according to plunger dimensions to ensure excusive shock and extrusion in challenging application. This engineered construction delivers the low friction characteristics of PTFE and graphite while providing superior abrasion resistance through high-strength Aramid reinforcement.

The dense braided structure ensures exceptional sealability by minimizing gaps and voids within the packing. When compressed, the packing forms a tight and reliable sealing barrier that effectively prevents fluid leakage even under demanding operating conditions.

HY 107 is designed to withstand high-pressure service while maintaining excellent dimensional stability and sealing integrity. Its outstanding resistance to abrasion, chemicals, Ammonia, and Carbamate solutions makes it suitable for a wide range of industrial applications where reliability, durability, and long service life are critical.

## 2. KEY FEATURES

- Multi-yarn construction combining Aramid filament and graphite-lubricated PTFE yarn

- Aramid reinforced corners provide exceptional abrasion resistance

- Graphite-lubricated PTFE faces ensure low friction operation

- Dense braid construction minimizes voids and enhances sealability

- Forms a tight sealing barrier under compression

- Designed for demanding pressure and temperature conditions

- Excellent durability in Ammonia and Carbamate service

- Wide chemical compatibility with various industrial media

- Conforms effectively to irregular sealing surfaces

- Tested and qualified as per EN 16752 for centrifugal pump sealing applications

## 3. PERFORMANCE ADVANTAGES

- Excellent abrasion resistance for extended service life

- Superior compression and recovery characteristics

- Performs effectively on worn, out-of-true shafts and spindles

- Excellent extrusion resistance under pressure

- Low shaft wear due to reduced friction characteristics

- High sealing efficiency under dynamic operating conditions

- Reliable performance in pumps, valves, and rotating equipment

- Long-lasting leak-free operation

- Reduced maintenance requirements and downtime

- Enhanced equipment protection and operational reliability

## 4. TECHNICAL PROPERTIES

| Property | Rotating | Reciprocating |  |
| --- | --- | --- | --- |
| pH Range | 1 – 13 | 1 – 13 |  |
| Temperature (°C) | -240 to +260 | -240 to +260 |  |
| Pressure (Bar) | 25 | 100 |  |
| Velocity (m/s) | 20 | 2 |  |
| Size Range | 6 mm² to 28 mm² |  |  |  |  |

## 5. CERTIFICATIONS

- Tested and qualified as per EN 16752 (Centrifugal Pumps Test Procedure for Seal Packing)

- Certified to Tightness Class T2

## 6. TYPICAL APPLICATIONS

- Centrifugal pumps

- Process pumps

- Industrial valves

- Agitators and mixers

- Chemical processing equipment

- Ammonia service applications

- Carbamate service applications

- General industrial rotating equipment

- Dynamic sealing applications

- Equipment handling abrasive media

## 7. SERVICE MEDIA

- Ammonia solutions

- Carbamate solutions

- Chemicals and solvents

- Water and wastewater

- Industrial process fluids

- Abrasive slurries

- Corrosive media

- General chemical process applications

## 8. PERFORMANCE BENEFITS

- Combines low friction operation with exceptional abrasion resistance

- Maintains sealing integrity under high pressure conditions

- Superior adaptability to irregular shaft and spindle conditions

- Excellent chemical resistance across a broad pH range

- Reduced shaft wear and equipment damage

- Outstanding durability in demanding industrial environments

- Reliable leak-free performance over extended service periods

- Reduced maintenance frequency and operating costs

- Enhanced equipment efficiency and operational reliability

- Suitable for critical industrial sealing applications

# DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.