## HY 120 AR

## An engineered Ramie Fibre Packing with alternate layer of aramid fibre, with PTFE impregnation for harsh industrial application.

## 1. PRODUCT OVERVIEW

INMARCO HY 120 AR is a premium-grade economical packing braided from extremely strong Ramie Fibre yarn and further impregnated with further reinforcement of strong aramid fibre enhance its chemical and abrasion resistance resulting in superior sealing performance.

The combination of natural Ramie fibres and aramid provide excellent abrasion resistance, reduced friction, and improved durability compared to conventional cotton fibre packings. Its dense construction allows optimum retention of lubricants and dispersants, resulting in superior sealing performance and extended service life.

HY 120 AR offers an economical alternative to synthetic packings and is particularly suitable for water handling mind particles e.g., industrial application containing sea water and marine industry where reliability and cost-effectiveness are essential.

## 2. KEY FEATURES

● Braided from high-strength Aramid and Ramie Fibre yarn.

● PTFE dispersion impregnation enhances chemical resistance.

● Superior resistance to mechanical wear compared to cotton fibre packing.

● Low friction characteristics reduce shaft and sleeve wear.

● High-density construction ensures improved saleability.

● Excellent penetration and abrasion resistance.

● Economical alternative to synthetic packing materials.

● Reliable sealing performance in water-based applications.

## 3. PERFORMANCE ADVANTAGES

● Improved wear resistance under continuous service conditions.

● Reduced friction for smoother equipment operation.

● Excellent dimensional stability during operation.

● Superior sealing performance through optimum dispersant retention.

● Cost-effective solution for general industrial services.

● Suitable for marine and water handling applications.

● Extended packing life under abrasive operating conditions.

● Reduced maintenance and replacement frequency.

## 4. TECHNICAL PROPERTIES

| Property | Value |
| --- | --- |
| pH Range | 6 – 11 |
| Temperature Range | -40°C to +150°C |
| Size Range | 3 mm² to 35 mm² |

## 5. SERVICE MEDIA

• Fresh Water

• Sewage Water

• Saline Water

• Turbid Water

• DM Water

• General Water Services

## 6. TYPICAL APPLICATIONS

• Equipment handling crystallizing fluids

• Marine stern tubes

• Rudder posts

• Bilge pumps

• Water wheel glands

• General water handling equipment

• Industrial pumps

• Marine service equipment

## 7. PERFORMANCE BENEFITS

● Better resistance to mechanical wear than conventional vegetable fibre packings.

● PTFE impregnation improves chemical resistance and lubrication.

● Low friction characteristics help minimize equipment wear.

● Dense construction promotes effective sealing performance.

● Excellent abrasion resistance for longer service life.

● Cost-effective replacement for many synthetic packing solutions.

● Suitable for demanding marine and water service applications.

● Reliable sealing with reduced maintenance requirements.

## DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.