# STYLE HY 510 EC

## High-Performance Hybrid Packing for Marine and Industrial Applications

## 1. PRODUCT OVERVIEW

INMARCO HY 510EC is a high-performance hybrid packing designed for demanding industrial and marine applications. It is manufactured from PTFE-based fibers with graphite incorporated into the molecular structure and reinforced with Aramid yarn with a hollow elastomer core.

This advanced construction delivers reliable sealing, dimensional stability, and extended service life, particularly in seawater and other demanding process media. Its optimized mechanical design ensures dependable leak-free operation under harsh operating conditions while protecting equipment from wear and thermal damage.

HY 510EC is tested and qualified as per EN 16752 (Centrifugal Pumps Test Procedure for Seal Packing), Tightness Class T2.

## 2. KEY FEATURES

● Manufactured from PTFE-based fibers with graphite incorporated into the molecular structure.

● Reinforced with Aramid yarn for enhanced mechanical strength and durability.

● Hollow elastomer core provides excellent resiliency and sealing performance.

● Adequate lubrication ensures low-friction operation and reduced equipment wear.

● Graphite content controls PTFE thermal expansion by approximately 20%, reducing the risk of overheating and extrusion.

● Excellent heat dissipation promotes cooler running and extended packing life.

● Does not cause embrittlement, abrasion, or erosion of shafts and sleeves.

● Specifically engineered for marine and industrial sealing applications.

● Tested and qualified according to EN 16752 Tightness Class T2.

## 3. PERFORMANCE ADVANTAGES

● Reliable sealing performance under demanding operating conditions.

● Excellent chemical resistance across a broad range of industrial media.

● Superior dimensional stability during continuous operation.

● Reduced friction resulting in lower shaft and sleeve wear.

● Enhanced resiliency ensures consistent sealing performance.

● Excellent thermal management for cooler operating temperatures.

● Particularly suitable for seawater applications.

● Long service life with reduced maintenance requirements.

● Dependable leak-free performance in critical applications.

● Optimized for rotating equipment operating in harsh environments.

## 4. TECHNICAL PROPERTIES

| Property | Value |
| --- | --- |
| pH Range | 0 – 14 |
| Temperature Range | -240°C to +280°C |
| Pressure | 200 Bar |
| Velocity | 25 m/s |
| Size Range | 12 mm² to 50 mm² |

## 5. SERVICE MEDIA

• Organic acids

• Inorganic acids

• Alkalis

• Organic chemicals

• Hot water

• Cold water

• DM water

• Seawater

• Condensate

• Solvents

• Alcohols

• Aldehydes

• Ketones

• Dyes

• General industrial chemicals

## 6. TYPICAL APPLICATIONS

• Pumps

• Agitators

• Dryers

• Mixers

• Reactor shafts

• Stern tubes

• Marine rotating equipment

• Industrial rotating equipment

## 7. PERFORMANCE BENEFITS

● PTFE-based fibers with graphite provide excellent chemical resistance and low friction characteristics.

● Aramid reinforcement enhances mechanical strength and dimensional stability.

● Hollow elastomer core improves resiliency and sealing efficiency.

● Graphite controls PTFE thermal expansion, reducing overheating and extrusion risks.

● Excellent heat dissipation promotes cooler operation and longer packing life.

● Protects shafts and sleeves from abrasion and wear.

● Delivers reliable performance in marine and seawater applications.

● Supports extended service life with reduced maintenance requirements.

● Provides dependable leak-free sealing in critical industrial services.

● Ideal for demanding rotating equipment applications.

## COMPLIANCE

Test Standard: EN 16752
Application: Centrifugal Pumps Test Procedure for Seal Packing
Tightness Class: T2

## DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.