# Style HY 801

## Versatile Packing with Superior Chemical and Thermal Resistance

## Style HY 801

HY 801 is a versatile hybrid packing manufactured from Non-Metallic Expanded Pure Graphite Yarn reinforced with high-structural Carbon Filament. The packing offers exceptional chemical resistance, thermal conductivity, and sealing performance in demanding industrial applications.

Impregnated with proprietary THERMOLUBE™ Graphite-Based Dispersion and an Inorganic Passive Corrosion Inhibitor, HY 801 protects equipment against galvanic corrosion while minimizing oxidation and loss on ignition.

The packing adapts easily to surface irregularities, ensuring smooth operation, excellent dry-run capability, and reliable sealing performance across a wide range of pumps and valves.

HY 801 is chemically inert, self-lubricating, and tested for fire-safe and corrosion-resistant applications.

## Key Features

● Manufactured from Non-Metallic Expanded Pure Graphite Yarn reinforced with high-structural Carbon Filament

● Each yarn and all four corners are reinforced with Carbon Filament for enhanced mechanical strength

● Excellent chemical resistance across a broad range of industrial media

● Superior thermal conductivity for efficient heat dissipation

● Self-lubricating construction minimizes shaft and stem wear

● Non-sticky material that does not corrode or erode parent equipment

● Chemically inert and does not leach contaminants into process media

● Suitable for use in pumps, valves, mixers, agitators, and other sealing applications

● Adopts to stuffing box irregularities for improved sealing performance

● Can also be utilized as an anti-extrusion ring

## Technical Specifications

### Technical Properties

| Properties | Rotating | Reciprocating |
| --- | --- | --- |
| pH Range | 0 – 14 | 0 – 14 |
| Temperature (°C) | -200 to +650 | -200 to +650 |
| Temperature (Non-Oxidizing Media) | Up to 2750°C | Up to 2750°C |
| Pressure (Bar) | 150 | 450 |
| Velocity (m/s) | 25 | 20 |
| Size Range | 6 sq. mm to 50 sq. mm | 6 sq. mm to 50 sq. mm |

## Performance Benefits

● Exceptional chemical resistance to a wide variety of aggressive media

● High thermal conductivity promotes efficient heat dissipation and cooler operation

● Low oxidation rate contributes to extended packing service life

● Suitable for both dynamic and static sealing applications

● Fire-safe construction for critical and fire-rated applications

● Excellent dry-run capability reduces equipment wear

● Adapts easily to surface irregularities for improved sealing efficiency

● Helps prevent galvanic corrosion through Inorganic Passive Corrosion Inhibitor technology

● Self-lubricating characteristics reduce shaft and stem damage

## Certifications & Testing

● Tested and certified as per API 607 Fire Safe Test

● Corrosion tested as per ASTM B117

## Typical Applications

● Pumps

● Mixers

● Agitators

● Reactors

● General industrial sealing services

## DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.