# IN 140

## Fiberglass Braided Packing

## 1. PRODUCT OVERVIEW

INMARCO Style IN 140 is a dry non-asbestos cover-on-cover braided packing manufactured from inorganic fibrous material based on refractory oxides. The packing offers excellent resistance to high temperatures and provides outstanding thermal and electrical insulation properties.

IN 140 is designed for static sealing applications operating under severe thermal conditions. The packing combines excellent thermal stability, chemical resistance, and mechanical resilience, making it suitable for a wide range of industrial sealing and insulation applications.

The product is fire retardant and certified as per IS 11871 method A and B (vertical and inclined flammability and UL 94 flammability). It is resistant to all types of gases, including flue gases, and exhibits excellent moisture resistance by repelling water rather than absorbing it.

The packing is non-toxic, non-hazardous, and environmentally friendly, ensuring safe handling and operation in industrial environments.

## 2. KEY FEATURES

● Manufactured from inorganic refractory oxide fibres

● Dry non-asbestos cover-on-cover braided construction

● Excellent thermal insulation properties

● Excellent electrical insulation characteristics

● High resistance to thermal degradation

● Fire retardant construction

● Resistant to flue gases and industrial gases

● Water repellent and moisture resistant

● Non-toxic and environmentally friendly

● Suitable for static sealing applications

## 3. PERFORMANCE ADVANTAGES

● Exceptional resistance to high operating temperatures

● Excellent thermal and electrical insulation performance

● Superior flame resistance and fire safety properties

● High resilience under continuous thermal exposure

● Resistant to chemical attack from a wide range of industrial media

● Does not absorb water, ensuring long-term dimensional stability

● Reliable sealing performance in severe industrial environments

● Maintains integrity under prolonged high-temperature operation

## 4. TECHNICAL PROPERTIES

| Property | Value |
| --- | --- |
| Temperature Rating | Up to +650°C |
| Maximum Pressure | 100 kg/cm² |
| pH Range | 1 – 13 |
| Thermal Conductivity | 0.20 W/mK (at average 650°C) |
| Loss on Ignition | 1% Max. at 650°C |
| Available Sizes | 3 sq. mm to 90 sq. mm |

## 5. SERVICE MEDIA

• Superheated Steam

• Saturated Steam

• Dry Ash

• Non-Oxidizing Liquids

• Non-Oxidizing Gases

• Dyes

• Chemicals

• Flue Gases

## 6. TYPICAL APPLICATIONS

• Furnace Doors

• Oven Doors

• Boiler Doors

• Peep Holes

• Inspection Ports

• Flange Grooves

• Exhaust Steam Pipes

• Kilns

• High Temperature Static Sealing Applications

## 7. PERFORMANCE BENEFITS

● Provides excellent thermal insulation in high-temperature environments

● Reduces heat loss and improves energy efficiency

● Enhances workplace safety through fire-retardant construction

● Maintains sealing integrity under continuous thermal cycling

● Resists degradation from industrial gases and chemicals

● Water-repellent properties improve operational reliability

● Long service life with minimal maintenance requirements

● Environmentally friendly and safe to handle

● Suitable for critical static sealing and insulation duties

## 8. COMPLIANCE

Fire Retardant and certified as per IS 11871 method A and B (vertical and inclined flammability and UL 94 flammability).

## DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.