# INMATEX™ 1400

## Expanded PTFE Sheet for High-Integrity Flange Sealing

## Product Description

INMARCO INMATEX™ TYPE 1400 is a premium expanded PTFE sheet manufactured from 100% virgin Polytetrafluoroethylene (PTFE) using an advanced expansion process. The material is soft, flexible, and highly resilient, allowing excellent compressibility and conformance to flange sealing surfaces.

The sheet exhibits outstanding resistance to creep, hot flow, and cold flow while maintaining excellent sealing performance under low bolt loads. Its unique expanded PTFE structure provides superior permeation resistance, emission control, and long-term sealing reliability across a wide range of chemical and industrial applications.

INMATEX™ 1400 withstands compressive loads exceeding 1650 bar, making it suitable for demanding sealing applications involving fragile and non-metallic flanges.

## Key Features

● Manufactured from 100% Virgin PTFE with ultra-high molecular weight fine resin

● Highly expanded structure provides exceptional flexibility and compressibility

● Excellent conformity to irregular flange sealing surfaces

● Resistant to creep, hot flow, and cold flow

● High sealing performance with minimum bolt torque

● Easy installation resulting in reduced downtime

● Excellent permeation and emission resistance

● Withstands compressive loads above 1650 bar

● Chemically inert and suitable for a broad range of aggressive media

● Suitable for fragile and sensitive flange materials

## Typical Applications

● Glass-lined equipment flanges

● FRP (Fiberglass Reinforced Plastic) flanges

● Ceramic flanges and joints

● Plastic piping systems

● Lined pipe joints

● Chemical process equipment

● Acid and alkali handling systems

● HCL processing plants

● PVC manufacturing facilities

● Nuclear industry applications

● General industrial fluid and gas sealing services

## Technical Specifications

### Technical Properties

| Property | Value |
| --- | --- |
| Material | 100% PTFE (Polytetrafluoroethylene) |
| Resin Type | Ultra High Molecular Weight Fine Resin |
| Fillers / Binders | None |
| Process | Highly Expanded |
| Colour | White |
| Thickness Tolerance | ±0.010" |
| Temperature Range | -267.77°C to +315.55°C |
| Pressure Range | Full Vacuum to 3000 PSI |
| Chemical Compatibility | pH 0 – 14 |
| Specific Gravity (ASTM D792) | 0.80 ± 0.10 |
| ASTM Testing | Yes |
| FSA Testing | Yes |

### Physical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Compressibility | ASTM F-36 | 66% |
| Recovery | ASTM F-36 | 12% |
| Creep Relaxation | ASTM F-38 | 38% |
| Matrix Tensile Strength | ASTM F-152 | 2106 PSI |
| Tensile Strength | ASTM F-152 | 5455 PSI |
| Elongation | ASTM F-152 | 169.9% |
| Tensile at Break Point | ASTM F-152 | 2632 PSI |

### Sealability Data

| Property | Value |
| --- | --- |
| Sealability – Fuel A (Isooctane) ASTM F-37-B | 0.02 ml/hr |
| Sealability – Fuel B (Nitrogen @ 60 psig) ASTM F-37-B | N/A |

### Thermal Performance

| Property | Value |
| --- | --- |
| Hot Compression Test | 300°C |
| Hot Loss | 70.9% |
| Hot Creep | 17.5% |

### FSA High Pressure Steam Test

| Test Condition | Result |
| --- | --- |
| 275°C @ 860 PSI for 561 Hours | Pass |
| Weight Loss | 0.49% |

## Performance Benefits

● Exceptional compressibility for sealing irregular flange surfaces

● Excellent recovery characteristics for long-term sealing reliability

● Superior resistance to creep relaxation and cold flow

● High tensile strength for enhanced durability and handling

● Excellent chemical resistance across the full pH range (0–14)

● Suitable for both liquid and gaseous media

● Low seating stress requirements reduce flange loading

● High sealing efficiency with minimum installation torque

● Outstanding permeation and emission control

● Resistant to aging, hardening, and degradation during service

● Reliable performance under vacuum and high-pressure conditions

● Ideal for fragile flanges including glass, FRP, ceramic, plastic, and lined equipment

## DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.