# NA 420

### Compressed Non-Asbestos Fiber Jointing Sheet

NA 420 is a high-quality compressed non-asbestos fiber (CNAF) jointing sheet manufactured from a blend of mineral fibers, aramid fibers, and inorganic fillers bonded with a high-performance NBR binder. It is designed to provide reliable sealing performance in medium-stress applications involving oils, fuels, steam, water, gases, hydrocarbons, and a wide range of industrial chemicals.

The material offers excellent tensile strength, recovery, gas tightness, and resistance to oils and fuels. Its balanced combination of mechanical strength and sealing capability makes it suitable for general industrial gasket applications where dependable performance and durability are required.

## Key Features

● Manufactured from a premium blend of mineral fibers, aramid fibers, and inorganic fillers with an NBR binder.

● Excellent tensile strength ensures reliable performance under mechanical loading conditions.

● High recovery characteristics maintain gasket integrity and sealing effectiveness during pressure fluctuations.

● Low stress relaxation provides long-term sealing stability and reduced maintenance requirements.

● Superior gas sealability minimizes leakage and enhances operational safety.

● Excellent resistance to oils, fuels, lubricants, steam, water, and hydrocarbons.

● Suitable for medium-stress sealing applications across a wide range of industrial systems.

● Available in multiple thicknesses and sheet sizes to suit various gasket manufacturing requirements.

## Applications

● General industrial gasket applications.

● Pumps, compressors, and pipe flanges.

● Oil and fuel handling systems.

● Steam and water service applications.

● Cooling water systems.

● Hydrocarbon processing equipment.

● Chemical processing systems handling diluted acids and alkalis.

● Industrial equipment requiring reliable sealing under medium pressure and temperature conditions.

## Technical Specifications

### Technical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Density (g/cm³) | ASTM F 1315 | 1.60 – 1.90 |
| Compressibility (%) | ASTM F 36 J | 7 – 17 |
| Recovery (%) | ASTM F 36 J | ≥ 50 |
| Tensile Strength (N/mm²) | ASTM F 152 | ≥ 9.50 |
| Maximum Peak Temperature (°C) | - | 300 |
| Maximum Operating Temperature (°C) | - | 220 |
| Maximum Operating Pressure (bar) | - | 80 |

### Availability

| Property | Value |
| --- | --- |
| Sheet Size | 1500 mm × 1500 mm, 1500 mm × 3000 mm |
| Thickness | 0.5, 0.8, 1.0, 1.5, 2.0, 2.5, 3.0, 4.0 & 5.0 mm |

## Performance Benefits

✓ Excellent sealing performance for oils, fuels, steam, water, gases, and hydrocarbons.

✓ High tensile strength ensures durability in demanding industrial environments.

✓ Superior recovery characteristics maintain seal integrity under fluctuating loads.

✓ Low stress relaxation improves long-term gasket reliability.

✓ Excellent resistance to oil and fuel absorption.

✓ High gas tightness minimizes leakage and improves process safety.

✓ Suitable for medium-pressure applications up to 80 bar.

✓ Available in a wide range of thicknesses and sheet sizes for flexible gasket fabrication.

✓ Cost-effective sealing solution for general industrial applications.

### Important Note

Gaskets should not be subjected to maximum temperature and maximum pressure simultaneously.