# NA 430

### Premium Non-Asbestos Fiber Jointing Sheet for High-Performance Sealing

NA 430 is a premium compressed non-asbestos fiber jointing sheet reinforced with SS304 stainless steel wire mesh for enhanced mechanical strength and dimensional stability. Manufactured using a high-performance calendaring process, it consists of high-tenacity aramid fibers blended with organic fibers and bonded with NBR.

The stainless steel wire mesh reinforcement improves pressure resistance, durability, and gasket integrity under demanding operating conditions. NA 430 is designed for medium- to high-stress sealing applications involving oils, fuels, steam, water, hydrocarbons, and a wide range of industrial chemicals.

## Key Features

● Reinforced with SS304 stainless steel wire mesh for superior mechanical strength and dimensional stability.

● Manufactured from high-tenacity aramid fibers and organic fibers bonded with premium NBR rubber.

● Excellent tensile strength ensures reliable performance under demanding operating conditions.

● High compressibility and recovery characteristics provide effective sealing and gasket resilience.

● Low stress relaxation helps maintain sealing load over extended service periods.

● Superior gas sealability minimizes leakage and improves operational safety.

● Excellent resistance to oils, fuels, lubricants, hydrocarbons, steam, and cooling liquids.

● Suitable for medium- and high-stress industrial sealing applications.

● Available in a range of sheet sizes and thicknesses to meet diverse gasket manufacturing requirements.

## Applications

● Pumps, compressors, and pipe flange connections.

● Oil and fuel processing systems.

● Steam and hot water applications.

● Petrochemical and chemical processing equipment.

● Hydrocarbon handling systems.

● Cooling water circuits and utility services.

● Industrial machinery requiring high-performance gasket materials.

● Applications involving diluted acids, alkalis, lubricants, and industrial fluids.

## Technical Specifications

### Technical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Density (g/cm³) | ASTM F 1315 | 1.70 – 2.00 |
| Compressibility (%) | ASTM F 36 I | 7 – 17 |
| Recovery (%) | ASTM F 36 J | ≥ 40 |
| Tensile Strength (N/mm²) | ASTM F 152 | ≥ 13.7 |
| Maximum Peak Temperature (°C) | - | 400 |
| Maximum Operating Temperature (°C) | - | 300 |
| Maximum Operating Pressure (bar) | - | 120 |

## Availability

| Property | Value |
| --- | --- |
| Sheet Size | 1500 mm × 1500 mm, 1500 mm × 3000 mm |
| Thickness | 1.0, 1.5, 2.0, 2.5, 3.0, 4.0 & 5.0 mm |

## Performance Benefits

● SS304 wire mesh reinforcement provides enhanced mechanical strength and blowout resistance.

● High tensile strength ensures durability under pressure and thermal cycling.

● Excellent recovery characteristics maintain gasket integrity during fluctuating operating conditions.

● Low stress relaxation improves long-term sealing reliability.

● Superior resistance to oils, fuels, hydrocarbons, steam, and cooling liquids.

● Excellent gas tightness minimizes leakage and enhances process safety.

● Suitable for operating pressures up to 120 bar.

● Performs reliably at temperatures up to 300°C, with peak resistance up to 400°C.

● Ideal for medium- and high-stress industrial sealing applications.

## Service Range

NA 430 is a premium metallic-grade gasket sheet suitable for oils, fuels, lubricants, alcohols, hydrocarbons, steam, water, cooling liquids, and most diluted acids and alkalis under medium-stress operating conditions.

For applications falling outside the recommended pressure-temperature operating range, please consult the INMARCO Technical Department.

### Important Note

Gaskets should not be subjected to maximum temperature and maximum pressure simultaneously.