# NA 432

### Advanced Non-Asbestos Fibre Sheet with Superior Chemical Resistance

NA 432 is a compressed non-asbestos fibre jointing sheet designed for general-purpose industrial sealing applications. It is manufactured from organic fibres bonded with high-quality NBR, providing reliable sealing performance, good compressibility, and excellent resistance to oils, fuels, water, and steam.

Complying with BS 7531 Grade Z, NA 432 offers a balanced combination of strength, flexibility, and sealing capability, making it suitable for medium-stress applications across a wide range of industrial equipment and piping systems.

## Key Features

● Manufactured from premium organic fibres bonded with NBR (Nitrile Butadiene Rubber).

● Complies with BS 7531 Grade Z specifications.

● Excellent compressibility enables effective sealing on irregular flange surfaces.

● Good recovery properties help maintain sealing integrity during pressure fluctuations.

● Low stress relaxation contributes to long-term gasket reliability.

● Superior gas sealability minimizes leakage and improves operational safety.

● Resistant to oils, fuels, water, and steam.

● Suitable for general-purpose industrial sealing applications.

● Available in multiple sheet sizes and thicknesses for versatile gasket fabrication.

## Applications

● General industrial gasket applications.

● Pumps, compressors, and pipe flanges.

● Oil and fuel systems.

● Steam and hot water services.

● Water treatment and utility systems.

● Low- to medium-pressure industrial equipment.

● General sealing applications requiring reliable and economical gasket materials.

## Technical Specifications

### Technical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Density (g/cm³) | ASTM F 1315 | 1.69 – 1.90 |
| Compressibility (%) | ASTM F 36 J | 7 – 17 |
| Recovery (%) | ASTM F 36 J | ≥ 40 |
| Tensile Strength (N/mm²) | ASTM F 152 | ≥ 7 |
| Maximum Peak Temperature (°C) | - | 200 |
| Maximum Operating Temperature (°C) | - | 150 |
| Maximum Operating Pressure (bar) | - | 50 |

## Availability

| Property | Value |
| --- | --- |
| Sheet Size | 1500 mm × 1500 mm, 1500 mm × 3000 mm |
| Thickness | 0.5, 0.8, 1.0, 1.5, 2.0, 2.5, 3.0, 4.0 & 5.0 mm |

## Performance Benefits

● Excellent compressibility allows effective sealing even on slightly uneven flange surfaces.

● Good recovery characteristics maintain gasket performance during pressure and temperature variations.

● Low stress relaxation improves long-term sealing reliability.

● Superior gas sealability minimizes leakage and enhances operational safety.

● Resistant to oils, fuels, water, and steam commonly encountered in industrial services.

● Complies with BS 7531 Grade Z requirements for dependable performance.

● Suitable for medium-stress applications up to 50 bar operating pressure.

● Cost-effective sealing solution for general industrial service conditions.

● Available in a wide range of thicknesses for custom gasket fabrication.

## Service Range

NA 432 is suitable for use with oil, steam, fuel, water, and other common industrial media. It is recommended for general-purpose sealing applications operating under medium pressure and temperature conditions.

If the application falls outside the recommended pressure-temperature operating range, please consult the INMARCO Technical Department.

### Important Note

Gaskets should not be subjected to maximum temperature and maximum pressure simultaneously.