## NA 442

### High-Temperature Non-Asbestos Fibre Sheet for Extreme Applications

NA 442 is a premium compressed non-asbestos carbon-filled gasket sheet manufactured using carbon fibres bonded with NBR. The carbon Fibre reinforcement significantly enhances the material's performance under high-temperature and high-pressure operating conditions.

Manufactured to BS 7531 Grade Y, NA 442 provides excellent sealing reliability, superior stress relaxation characteristics, and long-term mechanical stability in demanding industrial applications involving steam, hydrocarbons, oils, gases, and aggressive process media.

## Key Features

● Carbon Fibre reinforced construction provides superior performance in high-temperature and high-pressure applications.

● Manufactured using premium non-asbestos fibers with NBR binder for reliable sealing performance.

● Excellent tensile strength ensures mechanical integrity under demanding operating conditions.

● Superior recovery properties maintain gasket resilience during pressure cycling.

● Outstanding stress relaxation performance supports long-term sealing reliability.

● Low gas permeability minimizes leakage and improves operational safety.

● Suitable for a wide range of industrial fluids including steam, hydrocarbons, oils, gases, and chemicals.

● Complies with BS 7531 Grade Y requirements.

## Applications

● Hydrocarbons

● Steam and Water Systems

● Lubricants and Industrial Oils

● Mild Acids and Alkalis

● Alcohols and Solvents

● Industrial Gases

● Petrochemical and Chemical Processing Plants

● Power Generation Facilities

● General Industrial Flanged Connections

## Technical Specifications

### Technical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Density (g/cm³) | ASTM F 1315 | 1.69 – 1.90 |
| Compressibility (%) | ASTM F 36 J | 7 – 17 |
| Recovery (%) | ASTM F 36 J | ≥ 40 |
| Tensile Strength (N/mm²) | ASTM F 152 | ≥ 8 |
| Maximum Peak Temperature | — | 440°C |
| Maximum Operating Temperature | — | 350°C |
| Maximum Operating Pressure | — | 100 bar |

## Availability

| Property | Value |
| --- | --- |
| Sheet Size | 1500 mm × 1500 mm, 1500 mm × 3000 mm |
| Thickness | 0.5, 0.8, 1.0, 1.5, 2.0, 2.5, 3.0, 4.0 & 5.0 mm |

## Performance Benefits

● Carbon Fibre reinforcement enhances high-temperature and high-pressure performance.

● Excellent sealing capability with low gas leakage rates.

● High stress relaxation resistance ensures long-term sealing integrity.

● Good resistance to oils, fuels, hydrocarbons, steam, and water.

● Suitable for demanding industrial service conditions.

● Maintains dimensional stability under thermal and pressure cycling.

● BS 7531 Grade Y compliant material for quality assurance.

● Reliable performance across a broad range of industrial applications.

## Service Notes

Note: Gaskets should not be subjected to maximum temperature and maximum pressure simultaneously. For applications operating in extreme conditions, consult Inmarco technical support for material selection and suitability.