## NA 450

### Oil-Resistant Non-Asbestos Fibre Sheet for Industrial Sealing

NA 450 is a high-quality compressed non-asbestos Fibre jointing sheet manufactured from premium aramid Fibres, mineral Fibres, and NBR binder. Designed for reliable sealing performance in medium to high-stress industrial applications, NA 450 provides excellent mechanical strength, oil resistance, recovery characteristics, and long-term sealing stability.

Manufactured in compliance with BS 7531 Grade Y, the material is suitable for a wide range of industrial media including oils, fuels, hydrocarbons, steam, water, cooling liquids, alcohols, and diluted acids and alkalis.

## Key Features

● Premium aramid Fibre reinforcement provides excellent mechanical strength and durability.

● High-quality NBR binder offers superior resistance to oils, fuels, and hydrocarbons.

● Excellent tensile strength ensures reliable sealing performance under demanding service conditions.

● Superior recovery properties maintain gasket resilience and sealing integrity.

● Low creep and stress relaxation characteristics support long-term gasket performance.

● Excellent gas sealability minimizes leakage and improves operational safety.

● Suitable for a broad range of industrial fluids and process media.

● Manufactured in accordance with BS 7531 Grade Y standards.

## Applications

● Oils and Lubricants

● Fuels and Hydrocarbons

● Steam and Water Systems

● Cooling Liquids

● Alcohols and Solvents

● Industrial Gases

● Diluted Acids and Alkalis

● Pumps, Compressors, and Pipe Flanges

● Petrochemical, Chemical Processing, and General Industrial Applications

## Technical Specifications

### Technical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Density (g/cm³) | ASTM F 1315 | 1.69 – 1.90 |
| Compressibility (%) | ASTM F 36 J | 6 – 14 |
| Recovery (%) | ASTM F 36 J | ≥ 50 |
| Tensile Strength (N/mm²) | ASTM F 152 | ≥ 10.5 |
| Maximum Peak Temperature | — | 350°C |
| Maximum Operating Temperature | — | 250°C |
| Maximum Operating Pressure | — | 100 bar |

## Availability

| Property | Value |
| --- | --- |
| Sheet Size | 1500 mm × 1500 mm, 1500 mm × 3000 mm |
| Thickness | 0.5, 0.8, 1.0, 1.5, 2.0, 2.5, 3.0, 4.0 & 5.0 mm |

## Performance Benefits

● Premium aramid Fibre reinforcement provides enhanced strength and durability.

● Excellent oil, fuel, and hydrocarbon resistance for industrial sealing applications.

● Superior recovery characteristics maintain long-term gasket performance.

● Low creep relaxation improves sealing reliability under varying operating conditions.

● Excellent gas tightness minimizes fugitive emissions and leakage.

● Suitable for medium-stress applications across a wide range of industries.

● BS 7531 Grade Y compliant material ensures consistent quality and performance.

● Reliable performance under thermal and pressure cycling conditions.

## Service Notes

Note: Gaskets should not be subjected to maximum temperature and maximum pressure simultaneously. For critical operating conditions, consult Inmarco technical support for material selection and application suitability.