## NA 452 GF

### Glass Fibre Reinforced Non-Asbestos Sheet for Enhanced Strength

NA 452 GF is a premium compressed non-asbestos Fibre jointing sheet manufactured from aramid Fibre, glass Fibre, and NBR binder. The incorporation of glass Fibre reinforcement significantly improves mechanical strength, dimensional stability, temperature resistance, and sealing reliability under high-stress operating conditions.

Manufactured in compliance with BS 7531 Grade X, NA 452 GF is designed for demanding industrial sealing applications involving oils, fuels, hydrocarbons, steam, water, cooling liquids, diluted acids, alkalis, and various industrial process media.

## Key Features

● Premium glass Fibre reinforcement enhances mechanical strength and thermal stability.

● High-quality aramid Fibre construction provides excellent durability and sealing performance.

● Superior tensile strength ensures reliable operation under high-stress service conditions.

● Excellent recovery characteristics maintain sealing integrity during pressure fluctuations.

● Outstanding stress relaxation properties support long-term sealing reliability.

● Excellent resistance to oils, fuels, hydrocarbons, steam, and industrial chemicals.

● Low gas permeability minimizes leakage and improves operational safety.

● Manufactured in accordance with BS 7531 Grade X standards.

## Applications

● Oils and Lubricants

● Fuels and Hydrocarbons

● Steam and Water Systems

● Cooling Liquids

● Alcohols and Solvents

● Industrial Gases

● Diluted Acids and Alkalis

● Pumps, Compressors and Flanged Connections

● Petrochemical and Chemical Processing Plants

● Power Generation Facilities

● High-Stress Industrial Sealing Applications

## Technical Specifications

### Technical Properties

| Property | Test Method | Value |
| --- | --- | --- |
| Density (g/cm³) | ASTM F 1315 | 1.60 – 1.90 |
| Compressibility (%) | ASTM F 36 J | 5 – 15 |
| Recovery (%) | ASTM F 36 J | ≥ 50 |
| Tensile Strength (N/mm²) | ASTM F 152 | ≥ 10.5 |
| Maximum Peak Temperature | — | 450°C |
| Maximum Operating Temperature | — | 300°C |
| Maximum Operating Pressure | — | 120 bar |

## Availability

| Property | Value |
| --- | --- |
| Sheet Size | 1500 mm × 1500 mm, 1500 mm × 3000 mm |
| Thickness | 0.5, 0.8, 1.0, 1.5, 2.0, 2.5, 3.0, 4.0 & 5.0 mm |

## Performance Benefits

● Glass Fibre reinforcement improves mechanical strength and dimensional stability.

● Excellent resistance to oils, fuels, hydrocarbons, steam, and industrial chemicals.

● Superior stress relaxation characteristics ensure long-term sealing performance.

● High recovery properties maintain gasket resilience under pressure cycling.

● Low leakage rates improve process safety and efficiency.

● Suitable for high-stress sealing applications requiring reliable long-term service.

● BS 7531 Grade X compliant material ensures consistent quality and performance.

● Performs reliably across a broad range of industrial operating conditions.

## Service Notes

Note: Gaskets should not be subjected to maximum temperature and maximum pressure simultaneously. For critical operating conditions, consult Inmarco technical support for material selection and application suitability.