# OR 120

## Economical Ramie Fibre Packing with PTFE Dispersion for Enhanced Chemical Resistance

INMARCO Style OR 120 is a premium-grade economical packing braided from extremely strong Ramie fibre and impregnated with proprietary PTFE dispersion to enhance chemical resistance and sealing performance. The packing combines the natural strength of Ramie fibre with the lubricating and sealing properties of PTFE, making it a reliable and cost-effective solution for a wide range of industrial applications.

Its dense construction allows optimum retention of the PTFE dispersion, resulting in improved sealing efficiency, reduced leakage, and extended service life. OR 120 provides excellent abrasion resistance and mechanical durability while maintaining low friction during operation.

## Key Features

● Braided from high-strength Ramie fibre for excellent mechanical strength and durability.

● Impregnated with proprietary PTFE dispersion for enhanced chemical resistance.

● Better resistance to mechanical wear compared to conventional cotton fibre packings.

● Low friction characteristics reduce shaft and sleeve wear.

● High-density construction improves sealing efficiency and minimizes leakage.

● Excellent penetration and abrasion resistance for demanding applications.

● Cost-effective alternative to synthetic fibre packings.

● Suitable for a variety of water handling and marine applications.

## Applications

● Equipment handling crystallizing fluids

● Marine stern tubes

● Rudder posts

● Bilge pumps

● Water wheel glands

● Water treatment equipment

● General utility pumps

● Industrial water handling systems

## Service Media

● Fresh water

● Sewage water

● Saline water

● Turbid water

● Demineralized (DM) water

● Mild aqueous solutions

## Technical Specifications

| Properties | Rotating |
| --- | --- |
| pH Range | 6 – 11 |
| Temperature (°C) | -40 to +150 |
| Pressure (Bar) | 50 |
| Velocity (m/s) | 10 |
| Size | 3 sq mm to 35 sq mm |

## Performance Benefits

✓ Superior mechanical wear resistance compared to cotton fibre packings.

✓ Enhanced chemical resistance through PTFE dispersion impregnation.

✓ Low friction operation reduces shaft wear and power consumption.

✓ Dense construction improves sealing performance and leakage control.

✓ Excellent abrasion resistance for extended service life.

✓ Reliable performance in marine and water service applications.

✓ Economical replacement for synthetic packings.

✓ Easy installation and maintenance.

✓ Long-lasting sealing performance in demanding operating environments.

Note: OR 120 is specifically designed for water-based and marine applications where durability, abrasion resistance, and cost-effective sealing performance are essential.