# PE 104A

## High-Performance Sealing with the Strength of Aramid and the Softness of PTFE

INMARCO Style PE 104A is a high-performance gland packing developed for control valves operating in demanding industrial environments. It features a high-strength aramid yarn core that provides excellent mechanical strength, wear resistance, and durability. The outer PTFE jacket ensures low friction, smooth operation, and outstanding chemical compatibility across a wide range of process media.

Enhanced with fluoropolymer dispersion and corrosion inhibitors, PE 104A delivers long-lasting sealing performance even under severe operating conditions. Its advanced construction promotes efficient heat dissipation, minimizes leakage, and provides reliable sealing performance throughout its service life.

## Key Features

● Constructed around a high-strength aramid yarn core, providing exceptional resistance to wear, abrasion, and mechanical stress.

● Outer jacket of pure PTFE yarn ensures low-friction sealing and superior chemical compatibility.

● Treated with advanced fluoropolymer dispersion and corrosion inhibitors for enhanced durability and chemical resistance.

● PTFE suspensoid acts as a blocking agent, sealing micro-leakage paths and improving sealing efficiency.

● Conforms effectively to stuffing box irregularities for improved sealing performance.

● Allows quick installation and removal, reducing maintenance time and operational downtime.

● Suitable for both dynamic and static sealing applications.

## Applications

● Control valves

● Plug valves

● Process valves

● Hydrocarbon processing

● Chemical processing equipment

● Pharmaceutical plants

● Food processing industries

● Refineries and petrochemical plants

## Technical Specifications

| Property | Value |
| --- | --- |
| pH Range | 0 – 14 |
| Temperature (°C) | -240 to +260 |
| Pressure (Bar) | 300 |
| Size | 6.5 sq mm to 50 sq mm |

## Performance Benefits

● Exceptional dimensional stability for consistent sealing under varying operating conditions.

● Excellent resistance to wear, abrasion, and mechanical stress.

● Resists disintegration during operation, ensuring long-term reliability.

● Suitable for both dynamic and static sealing applications.

● Non-toxic and chemically inert, ideal for clean and sensitive environments.

● Low friction and reduced shaft wear due to PTFE dispersion and advanced lubrication.

● Effective heat dissipation helps maintain reliable sealing performance.

● Extended service life with minimal maintenance requirements.

● Reliable sealing across steam, hydrocarbons, acids, alkalis, solvents, and other industrial media.

Note: PE 104A combines the mechanical strength of aramid fiber with the chemical resistance and low-friction characteristics of PTFE, making it particularly suitable for demanding control valve and industrial sealing applications requiring long service life and dependable performance.