# PE 504

## High-Performance Packing for Industrial Service

Style PE 504 is manufactured from expanded PTFE with graphite, molecularly bonded to provide enhanced sealing performance. The unique combination delivers excellent chemical resistance, superior heat dissipation, and high resilience, resulting in extended service life and reliable operation in demanding industrial environments.

Its low-friction characteristics help minimize wear and erosion on shafts and sleeves while maintaining dimensional stability under varying operating conditions. Requiring minimal gland pressure, PE 504 performs efficiently at high speeds with low leakage rates. It is compatible with a wide range of industrial media, except strong oxidizers, molten alkali metals, and fluorine compounds.

The packing is ideally suited for pumps, valves, reactors, agitators, and other rotating equipment where dependable sealing and long-term reliability are required.

## Key Features

● Manufactured from expanded PTFE with graphite, molecularly bonded for enhanced performance.

● Excellent chemical resistance across a broad range of industrial media.

● Superior heat dissipation helps maintain cooler operating temperatures.

● Low-friction construction minimizes shaft and sleeve wear.

● High resilience and dimensional stability ensure long-term sealing reliability.

● Requires minimal gland pressure for effective sealing.

● Performs efficiently in high-speed applications with low leakage.

● Suitable for dynamic and static sealing applications.

● Tested and qualified as per EN 16752 (Centrifugal Pumps – Test Procedure for Seal Packing), Tightness Class T1.

## Applications

● Centrifugal pumps

● Rotary pumps

● Agitators

● Mixers

● Reactors

● Process equipment

● High-speed rotary systems

● Chemical processing industries

● General industrial sealing applications

## Technical Specifications

### Technical Properties

| Properties | Rotating | Reciprocating |
| --- | --- | --- |
| pH Range | 0 – 14 | 0 – 14 |
| Temperature (°C) | -200 to +300 | -200 to +300 |
| Pressure (Bar) | 100 | 200 |
| Velocity (m/s) | 25 | 10 |
| Size | 3 sq mm to 35 sq mm |  |

## Performance Benefits

● Engineered to perform reliably under demanding industrial operating conditions.

● Excellent chemical compatibility with a wide variety of process media.

● High thermal conductivity promotes efficient heat dissipation.

● Low friction characteristics reduce equipment wear and extend service life.

● Maintains sealing integrity with minimal leakage and reduced maintenance requirements.

● Suitable for high-speed rotary equipment and dynamic sealing applications.

● Exceptional dimensional stability under fluctuating temperatures and pressures.

● Provides long service life with dependable operational performance.

● Supports safe and efficient operation across multiple process industries.

### Certification

✓ Tested and qualified as per EN 16752 (Centrifugal Pumps – Test Procedure for Seal Packing), Tightness Class T1

Note: PE 504 is suitable for most industrial chemicals and media; however, it is not recommended for use with strong oxidizing agents, molten alkali metals, or fluorine compounds.