# 1. PRODUCT OVERVIEW

INMARCO Ring Type Joint (RTJ) Gaskets are precision-machined metallic sealing components engineered for critical high-pressure and high-temperature applications across offshore, onshore, petrochemical, refinery, and subsea industries.

Designed for metal-to-metal sealing reliability, RTJ gaskets provide exceptional sealing integrity under severe pressure, thermal cycling, vibration, and corrosive operating conditions. The self-energizing sealing principle improves gasket performance as internal pressure increases, making RTJ gaskets highly suitable for wellhead systems, pressure vessels, subsea pipelines, and critical flange connections.

Manufactured in accordance with API 6A and ASME B16.20 standards, INMARCO RTJ gaskets are available in Oval, Octagonal, RX, and BX profiles to suit various flange groove configurations and service conditions.

The gasket materials are carefully selected to ensure compatibility with flange hardness, process media, temperature conditions, and corrosion resistance requirements, ensuring reliable long-term sealing performance in demanding industrial applications.

# 2. KEY FEATURES

- Precision-machined solid metal gasket construction

- Designed for extreme pressure and high-temperature sealing applications

- Reliable metal-to-metal sealing performance for critical industrial services

- Self-energizing sealing action improves sealing integrity under increasing pressure

- Available in Oval, Octagonal, RX, and BX profile configurations

- Excellent blowout resistance under severe operating conditions

- Suitable for offshore, subsea, refinery, and petrochemical applications

- Manufactured in accordance with API 6A and ASME B16.20 standards

- Wide range of metallurgy options for aggressive media compatibility

- High structural integrity for critical safety applications

- Custom dimensions and specialized alloy materials available upon request

# 3. RTJ PROFILE TYPES

### Type R – Oval

- Original RTJ gasket design with rounded profile configuration

- Suitable for both rounded-bottom and flat-bottom groove flanges

- Provides reliable sealing performance in standard high-pressure applications

- Fully compliant with ASME B16.20 and API 6A standards

### Type R – Octagonal

- Improved sealing profile with direct surface contact on 23° groove faces

- Offers enhanced sealing efficiency compared to oval profiles

- Fully interchangeable with Oval profile in flat-bottom groove applications

- Suitable for high-pressure and critical service environments

### Type RX

- Pressure-activated adaptation of the R-Octagonal design

- Outer sealing surfaces create initial contact and self-energizing sealing action

- Internal pressure further increases gasket sealing performance

- Designed for improved sealing reliability under elevated pressures

### Type BX

- Designed specifically for ultra-high-pressure applications up to 20,000 psi (1,380 bar)

- Compatible only with dedicated BX groove configurations

- Not interchangeable with R or RX groove designs

- Optional pressure equalization hole available for subsea applications

# 4. PERFORMANCE ADVANTAGES

- Excellent sealing integrity under extreme pressure conditions

- Superior resistance to blowout and extrusion failure

- Reliable sealing performance during thermal cycling and vibration

- High mechanical strength for severe industrial applications

- Suitable for aggressive chemical and hydrocarbon service environments

- Excellent dimensional stability under high compressive loads

- Reliable long-term sealing performance with reduced maintenance requirements

- Enhanced operational safety in critical process systems

- Compatible with high-pressure offshore and subsea applications

- Suitable for demanding EPC and OEM industrial requirements

# 5. TECHNICAL PROPERTIES

| Property | Specification |
| --- | --- |
| Construction | Precision-machined solid metallic ring gasket |
| Pressure Range | Up to 20,000 psi (1,380 bar) depending on profile and application |
| Temperature Range | -200°C to +800°C depending on material selection |
| Profile Types | Oval, Octagonal, RX, BX |
| Standards | API 6A, ASME B16.20 |
| Typical Sizes | 1/2" to 24" standard sizes, custom sizes available |
| Application Type | High-pressure flange sealing applications |
| Groove Compatibility | R, RX, BX flange groove configurations |

# 6. MATERIAL OPTIONS

| Material | Maximum Hardness (BHN) | Material Marking |
| --- | --- | --- |
| Soft Iron | 90 | D |
| Low Carbon Steel | 120 | S |
| 4–6% Cr / ½% Mo | 130 | F5 |
| 410 Alloy Steel | 170 | S410 |
| SS304 | 160 | S304 |
| SS304L | 160 | S304L |
| SS316 | 160 | S316 |
| SS316L | 160 | S316L |
| SS321 | 160 | S321 |
| SS347 | 160 | S347 |
| Monel | 135 | N04400 |
| Inconel 625 | On Request | 625 |
| Inconel 825 | On Request | 825 |
| Hastelloy C276 | On Request | C276 |
| Titanium | On Request | Ti |

# 7. APPLICATIONS

- Offshore oil & gas platforms

- Wellhead and Christmas tree equipment

- Subsea pipeline systems

- High-pressure refinery piping systems

- Petrochemical processing plants

- Pressure vessels and reactor systems

- High-pressure steam services

- LNG and gas processing facilities

- Critical hydrocarbon flange connections

- Power generation plants

- Safety-critical industrial process systems

# 8. PERFORMANCE BENEFITS

- Reliable sealing performance under extreme industrial operating conditions

- Improved operational safety in high-pressure applications

- Superior pressure handling capability compared to conventional gasket systems

- Reduced leakage and enhanced environmental compliance

- Excellent compatibility with critical hydrocarbon services

- Long operational life with reduced maintenance intervention

- High resistance to thermal shock and pressure fluctuations

- Enhanced sealing integrity for subsea and offshore installations

- Suitable for mission-critical EPC and industrial projects

- Supports safer, cleaner, and more reliable industrial operations

# 9. TESTING & VALIDATION

- Manufactured in accordance with API 6A and ASME B16.20 requirements

- Suitable for NACE MR0175 compliant service applications

- Precision-machined to stringent dimensional tolerances

- Designed for critical high-pressure industrial sealing applications

# DISCLAIMER

All technical information, recommendations, and performance data provided in this technical datasheet are based on current knowledge, laboratory testing, and industrial experience. Actual product performance may vary depending on operating conditions, equipment design, installation practices, process media, pressure, temperature, and application environment. Final product selection and suitability should be determined by the user based on the specific service conditions and application requirements.